Application of Transparent Soil Materials in Geotechnical Tunnel Model Tests(18pt, Times New Roman，bold)

LIU Hanlong1, ZHANG Huang1, XIAO Peng1, 3, ZHANG Wengang1, 2, SUN Weixin1,5, *, QI Rujian4, CHEN Zhen4(14pt, Times New Roman)

- School of Civil Engineering, Chongqing University, Chongqing 400045, China; 2. State Key Laboratory of Safety and Resilience of Civil Engineering in Mountain Area, Chongqing 400045, China; 3. Chongqing Railway Investment Group Co., Ltd., Chongqing 400023, China; 4. The First Engineering Co., Ltd. of China Railway Tunnel Group, Chongqing 401123, China; 5. College of Aerospace Engineering, Chongqing University, Chongqing 400044, China)(10.5pt, Times New Roman)

Abstract(10.5pt, Times New Roman, bold): Transparent soil techniques provide a visual medium and experimental approach for the testing of geotechnical tunnel models. However, most existing studies focus on individual material development or adaptations to specific working conditions, with systematic synthesis and comprehensive overviews remaining limited. This review discusses progress in transparent soil–based tunnel model testing from the perspectives of materials, optics, experimental applications, and evaluation. From the material perspective, we review the evolutionary development of transparent soil materials and summarize the compositional characteristics and physical–mechanical parameter matching principles of sand-type, clay-type, and rock-like transparent soils, emphasizing key issues related to material preparation and parameter adjustment. From the perspective of optics, we clarify the optical fundamentals of transparent soil model testing and discuss core components such as transparency requirements, model box size constraints, laser parameter selection, optical measurement techniques, and artificial speckle preparation while comparing the applicable ranges of digital image correlation and particle image velocimetry. From the experimental perspective, we systematically review representative applications of transparent soil materials in tunnel geotechnical model tests. These applications cover tunnel face stability, grouting diffusion, and construction-induced ground deformation. On this basis, experimental observations with potential transferability are identified. From the perspective of evaluation and outlook, several limitations are addressed, including constraints related to material equivalence, restrictions on model scale imposed by optical path length, insufficient speckle stability, and the high cost of experimental systems. Practical approaches to mitigating these problems are proposed (such as three-step equivalence calibration based on reactivity evaluation, guidance for selecting optical measurement techniques, and directions for the development of new transparent soil materials) to enhance engineering comparability and extrapolation capability under unprecedented working conditions.(10.5pt, Times New Roman)

Keywords(10.5pt, Times New Roman, bold): transparent soil; tunnel engineering; physical modeling test; particle image velocimetry; digital image correlation; speckle pattern preparation; stratum displacement field(10.5pt, Times New Roman)

DOI(9pt, SimHei)：10. 3973/ j. issn. 2096-4498. 2026. 01. 001 (9pt, FZShuSong-Z02S)

中图分类号(9pt, SimHei): U 45(9pt, FZShuSong-Z02S)　　　　　文献标志码(9pt, SimHei):A(FZShuSong-Z02S)　　　　  　文章编号(9pt, SimHei): 2096-4498(2026)01-0001-34(9pt, FZShuSong-Z02S)

透明土材料在隧道岩土工程模型试验中的应用综述(18pt,SimHei)

刘汉龙1，张煌1，肖鹏1，3，仉文岗1，2，孙伟鑫1，5，*，齐如见4，陈真4(14pt, KaiTi)

(1. 重庆大学 土木工程学院，重庆 400045；2. 重庆大学 山区土木工程安全与韧性全国重点实验室，重庆 400045；3. 重庆铁路投资集团有限公司，重庆 400023；4. 中铁隧道集团一处有限公司，重庆 401123；5. 重庆大学 航空航天学院，重庆 400044)(10.5pt, KaiTi)

摘要(9pt, SimHei)：透明土技术为隧道岩土工程模型试验提供了可视化介质与方法，但既有研究多聚焦于单一材料研发或特定工况适配，系统梳理与总览性说明仍显不足。本文围绕“材料—光学—试验应用—评估”四个维度，对以透明土材料为核心的隧道工程模型试验技术进行系统阐述：1)材料层面，梳理透明土材料研发的演进脉络，归纳砂土型、黏土型及类岩型透明土材料的组分特征及其物理力学参数匹配原则，提炼材料制备与调参的关键要素；2)光学层面，阐明透明土模型试验的光学基础，从透明土透明度、模型箱尺寸、激光器参数、光学测量技术与人工制斑技术等试验重要组分进行归纳，并比较DIC/PIV等测量方法的适用区间；3)试验层面，综合梳理透明土材料在隧道岩土工程模型试验中的典型应用实例，涵盖隧道开挖面稳定性、注浆扩散与施工诱发地层变形等研究，并提取可迁移应用的试验规律；4)评估与展望方面，指出透明土材料等效性的局限、透光性对模型尺度的约束、制斑稳定性不足以及试验系统成本较高等可能存在的发展问题；同时提出了适用于透明土材料的反应性评价指标的“等效性校准三步骤”、光学测量技术选用参考及新型透明土材料开发等实用方法与建议，以拓展其在应对前所未有之工况时的工程可比性与类推性。(9pt, FZShuSong-Z02S)

关键词(9pt, SimHei)：透明土；隧道工程；物理模型试验；粒子图像测速(PIV)；数字图像相关(DIC)；制斑技术；地层位移场(9pt, FZShuSong-Z02S)

Introduction

- (Heading 1, 12pt, Times New Roman, bold)

- (Text, 10.5 pt, Times New Roman)

More than a decade ago, China had already become the country with the largest number of highway tunnels and fastest rate of tunnel development[1]. This rapid expansion has been accompanied by the completion of technically demanding projects marking important milestones in tunnel engineering practice[2], as exemplified by the completion of the immersed tunnel of the Hong Kong–Zhuhai–Macao Bridge in 2017, world’s first extra-long twin-tube spiral tunnel (the Hankou Tunnel) in 2022, and Xiagongla Mountain Tunnel in October 2024. With a design elevation approaching 5000 m along its full length, the Xiagongla Tunnel has permanently eliminated seasonal traffic interruption caused by snow cover at what was once known as the most hazardous gateway to Tibet[3].

These projects not only demonstrate China’s growing technical capability in tunnel construction but also reflect a broader transition from large-scale construction to increasingly complex and condition-sensitive engineering practice.

The increasing scale and technical sophistication of tunnel projects have exposed challenges that cannot be resolved through experience-based design alone[4]. In practice, tunnel construction is strongly influenced by geological complexity and regional variability, which result in pronounced differences in deformation mechanisms, failure modes, and construction performance across projects. Although landmark works such as the immersed tunnel of the Hong Kong–Zhuhai–Macao Bridge demonstrate the feasibility of overcoming extreme engineering constraints, the direct replication of such construction strategies is rarely realistic under different geological and hydrological conditions.

Transparent soil material systems and development status

Overview of transparent soil materials

- (Heading 2, 10.5pt, Times New Roman, bold)

Research and development progress

    - (Heading 3, 10.5pt, Times New Roman)

Before the development of transparent soil testing materials, most experimental studies relied on embedded strain gauges and other sensor-based techniques, X-ray scanning, or marker tracing methods. These intrusive three-dimensional (3D) techniques generally exhibited limited spatial resolution and accuracy, particularly when applied to complex deformation processes within geomaterials[5]. As a result, the internal response of the soil mass could only be inferred indirectly.

Applications of transparent soil techniques

The development of transparent soil materials has been accompanied by that of experimental equipment and optical systems for transparent soil testing. He et al.[14] reviewed the evolution of transparent soil testing techniques and material configurations and explained the working principles of experimental apparatus for transparent geotechnical testing. Liu et al.[15] developed an optical slicing system for transparent soil model tests consisting of a laser light source, camera, frame grabber, and computer. Displacement fields were obtained using DIC to generate a commonly adopted optical configuration for transparent soil experiments.

Table 1 summarizes the transparent soil materials adopted in different physical model tests. Given that this comparison focuses on material selection and differences, the listed cases do not necessarily correspond to the first application of each material.

Table 1(9pt, Times New Roman, bold)　Materials used in transparent soil model tests(9pt, Times New Roman)

(Text in the table, 7.5pt, Times New Roman)

| References | Property type | Solid phase | Liquid phase | Test content |
| --- | --- | --- | --- | --- |
| Iskander et al. (1994)[6] | Clays and silts | Amorphous silica powder | White mineral oil and a normal-paraffinic solvent(calcium bromide and water) | Consolidation and triaxial compression tests |
| Iskander et al. (2002)[9] | Clay | Silicas with aggregate sizes of 1.4–175 μm | 1:1 (w/w) blend of Drakeol 35® mineral oil and Norpar 12® paraffinic solvent | Consolidation and triaxial compression tests |
| Yuan et al. (2021)[19] | Saturated solution soil | Glass sand | n-Dodecane and no. 15 white oil with a transparent pore solution | Displacement field of layered soils surrounding laterally loaded pile |
| Kong et al. (2020)[30] | Clay | Insoluble acrylic acid polymer | Water | Consolidation, penetration, and thermal conductivity tests |

Speckle preparation methods and application status

Speckle preparation methods

Zhou et al.[84] employed a 3D printing technique to fabricate transparent granular soils, achieving satisfactory speckle patterns without the addition of tracer particles (Fig. 1). This approach relies on intrinsic material heterogeneity to generate speckle patterns[85] and thereby eliminates the need for foreign additives but requires stringent control over material properties and laser parameters.

Fig. 1(9pt, Times New Roman, bold)　Laser-induced speckle field[84](9pt, Times New Roman,)

Conclusions and recommendations

Conclusions

This review provides a concise summary of transparent soil materials and the technical components involved in transparent soil physical model tests. Classic experimental cases using transparent soils to simulate different geomaterials are reviewed and analyzed, with particular focus placed on tunnel engineering. Particular attention is given to commonly used experimental equipment, transparent soil material preparation methods, and the results of representative tunnel model tests. In addition, several typical model design systems are introduced.

Recommendations

(1) Development of new transparent soil materials with enhanced applicability. Advances in material development can extend the current limits of experimental research and improve the consistency between model tests and actual engineering conditions. However, the currently available transparent soil materials remain limited and are insufficient to represent complex engineering geological environments. Moreover, natural strata are inherently anisotropic and heterogeneous, whereas most existing studies rely on available similar materials and explore different working conditions or experimental environments. Although the development of new transparent soil materials is highly challenging, progress in this area could help address issues such as small model size and limited general applicability.

The above discussion and recommendations reflect current issues and potential research directions related to the application and development of transparent soil techniques. Future transparent soil testing may place greater emphasis on material innovation, technical integration, cost control, and improved engineering applicability. This review is expected to encourage research on transparent soil model testing for tunnel engineering and support the gradual transition of this technique from laboratory studies to engineering practice.

- Acknowledgement

- (If has, reference to Heading 1, 12pt, Times New Roman，bold)

This study was supported by the National Major Scientific Instruments Development Project of China (No. 5202780029).

References:(9pt, Times New Roman，bold)

[1] Reporter for the journal of Tunnel Construction. China is already the country with the largest number of highway tunnels and the fastest development in the world: Jiang Shuping, Chairman of the Tunnel Engineering Branch of China Highway Society, Speech at the opening Ceremony of the 2013 National Highway Tunnel Academic Exchange Conference (excerpt) [J]. Tunnel Construction, 2013, 33 (10): 808.(9pt, Times New Roman)